Observed Adverse Chemical Reactions

Alumina and Graphite

- Eutectic point around 1800C

Magnesium Oxide and Alumina

- Leaves strange black marks on MgO

Magnesium Oxide and Tantalum

- Diminishes the quality of the susceptor (Very little visual indicators)

- Oxidizes tantalum and melts

YSZ and Boron Nitride (2500C)

- Changes the surface finish of the BN

Tantalum and Boron Nitride

- Changes surface color and finish and color of Ta

YSZ and Tantalum (2500C)

- In excess it changes the Ta to the color of Yttrium

- Diminishes the quality of the Susceptor

Carbon and Tantalum

- Turns the Ta gold colored, the TaC  very hard and appears to still be a good susceptor

Oxygen and anything